## Slide 1: NLH update 03/31/23

## Slide 2: Brute force approach—Pure NFL/NFH
Choose parameters for NFL and NFH independently
NFL Possibilities
NFH Possibilities
b: Kuhn length
v: Monomer volume
c: Flory Huggins parameter for
most hydrophobic residues
For example,

## Slide 3: Brute force approach—Blended NFL/NFH
Some examples at L100, L80, L30, L00; ignore points with H = 0
Even with many curves that look good for the pure cases, the height profiles are consistently very non-linear with respect to L composition (from top to bottom)
Experimental heights look more or less linear with respect to NFL addition

## Slide 4: If height profiles are linear with L, shouldn’t V_L = V_H?
For i as L or H,
i.e., Replacing a charged L chain with an equal volume of neutral H chain
Can control NFL and NFH volume with both the number of Kuhn monomers N_K and the volume of Kuhn monomers \nu_K:
If the height is controlled only by volume of charge, results should be similar regardless which parameter is changed
Changing b_L
Changing \nu_L
Still very nonlinear with L
There must be a conformational reason behind the non-linear response

## Slide 5: Volume fraction of the inner layer seems to saturate at \approx 0.80
L80 / H20
L30 / H70
H
L
L
H
H
L
L
H
Changing b_L (from prev. slide)
Changing \nu_L (from prev. slide)
The volume of both total protein (with respect to the grafting density) may be too high, pushing NFL out regardless of NFL/NFH properties

## Slide 6
Currently trying

## Slide 7: Phosphorylated NFH Progress
Currently running one more to get a closer fit; if not, the current best one should be close enough
These parameters are close to those of the native NFH. Hopefully means that I can use the final parameters of native NFL to get the blended phosph. results
Quick note: the points that go to zero just didn’t converge. The point at 6 nm takes a really long time to converge, so I will probably proceed with only calculating from 1 to 6 nm.
In the future, if needed, I can go to 8 nm (1.6 mM)
phosph. = - 1.5 e
Trials