## Slide 1: Structure and Phase Response of Neurofilament-Heavy Protein Brushes
Takashi Yokokura
Wang Group Meeting
04/01/2022

## Slide 2: Motivation – Polymer Brushes
Represent an extremely rich space within the polymer field, with or without embedded charge
Theoretical work pioneered by de Gennes (1980) and both theoretically and numerically progressed by
  Fleer, Leermakers (SFbox, Neurofilament)
  Borisov, Zhulina (Homopolymer & weak PE phase transitions, applications of SFbox)
Height (H)

## Slide 3: Motivation – Neurofilaments
Neurofilaments are protein brushes present within the axon of the neuron and determine the structural rigidity of the axon
  Found to be a common site of mutations within patients of neurodegenerative diseases such as Alzheimer’s Disease and Parkinson’s Disease.
Yuan, Rao, Nixon. (2012). Neurofilaments at a Glance. J Cell Sci. 125 (14): 3257–3263.
Figure Credit: Erika Ding

## Slide 4: Motivation – Neurofilaments
Our model was able to reproduced existing published SCF results on the internal structure
  Presented in my previous group meeting
Zhulina and Leermakers, Biophys. J., 93, 2007

## Slide 5: Overview
Model
  SCF derivation
  Charge distribution coarse-graining
NFH Brush
  Validation using Srinivasan et al., 2014
  Conformational behavior and structure
Extensions
  Multiple peaks
  Binary NF brush
  Local pH consideration
Conclusions

## Slide 6: Model – SCF Review
Goal: Adapt framework for free polyelectrolyte in solution to model end-grafted protein brushes in solution
Interactions:
  Elastic entropy following Gaussian statistics
  Flory-Huggins 2-body interactions
  Incompressibility
  Electrostatics, ignoring any correlations

## Slide 7: Model – SCF Review
Semicanonical partition function
  Canonical in polymer, grand canonical in ions and solvent
Particle-to-field transformations
Hubbard-Stratonovich transformation
Saddle-point approximation
Block copolymer approximation

## Slide 8: Model – SCF Review
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 9: Model – SCF Review
Satisfied Equations
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 10: Model – Coarse-graining Method
Coarse-graining performed by grouping charges based on contributions to the slope of the cumulative charge
  Hyperparameters: Number of bins, Minimum number of AA per block
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK

## Slide 11: Overview
Model
  SCF derivation
  Charge distribution coarse-graining
NFH Brush
  Validation using Srinivasan et al., 2014
  Conformational behavior and structure
Extensions
  Multiple peaks
  Binary NF brush
  Local pH consideration
Conclusions

## Slide 12: NFH Brush – Previous Experiment
Neurofilament-Heavy (NFH) sidearms grown by E. coli and grafted onto a planar surface as an “intrinsically disordered protein brush” for use as biomaterial (flow valves, smart sensors, etc.)
Measured height response at various pH and salt concentrations
All following results will be for the response to salt concentration at constant pH = 2.40
  Low and constant pH minimizes the amount of charge annealing in weak PE
Ongoing (separate) collaboration with Erika Ding, PhD Candidate in Kumar Group

## Slide 13: NFH Brush – Coarse Graining

## Slide 14: Corrected - 20220722
Old:

## Slide 15: NFH Brush – Experimental vs. Predicted
Very good match (excellent if metastable used)
  Sharp transition properly reproduced
Plot reports impossible ionic strengths given current pH
  At pH = 2.4,
  Extended curves give more insight into polymer conformation (as shown on next slide)

## Slide 16: NFH Brush – Conformational Competition
“C”, where denotes number of condensed regions
Condensed regions can exist with extended, diffuse regions
1C
2C

## Slide 17: NFH Brush – Phase Transition Order
2nd Order from Collapsed to Collapsed-Coil
  Globule to Coil
1st Order between 1C and 2C
  Sphere to Pearl-Necklace
1C
2C
2nd Order
2nd Order
1st Order

## Slide 18: NFH Brush – Internal Structure
What is the underlying structure of this new, phase segregated conformation?
Phases contain different chains
(expelled)
Segments “locked” into layers
Same chains in both phases (pn-like)
Segments can fluctuate between layers
Overall density profiles will look identical

## Slide 20: NFH Brush – Internal Structure
Block decomposition of 2C can discern between structures
2
1
3
4
5
6
7
1
2
3–7

## Slide 21: NFH Brush – Internal Structure
Same concept for dilute, coil phase
Previously demonstrated theoretically (for 1C only)
(Colors added to emphasize phase segregation, not to denote statistically distinguishable chains)
Adapted from Klushin, Birshtein, Amoskov. Macromolecules, 2001.

## Slide 22: NFH Brush – Internal Structure
How does internal structure affect response to salt concentration?
Dramatic collapse
Cooperative collapse

## Slide 23: Overview
Model
  SCF derivation
  Charge distribution coarse-graining
NFH Brush
  Validation using Srinivasan et al., 2014
  Conformational behavior and structure
Extensions
  Multiple peaks
  Binary NF brush
  Local pH consideration
Conclusions

## Slide 24: Extensions – C
Multi-peak profiles are preliminary, but suggest a much richer space than previously thought (no previous mention of multiple condensed layers that I could find)

## Slide 25: Extensions – Binary NF Brush
NF in biological systems contain a blend of H, M, L profiles
Why are compositions not consistent across location in the nervous system and neuronal development?
  How do the compositions affect accessible conformations?
  Do different compositions respond to stimuli differently?
Experimental collaborators can systematically measure height vs. binary (and ternary in the future) composition
(Preliminary data)

## Slide 26: Extensions – Local pH
Charge distribution of weak PE in dilute brushes (e.g. NF) are sensitive to local pH
For systems at low H+ concentration (e.g. physiological conditions), local pH differs significantly from bulk conditions
Local degree of dissociation
Brush electric potential
Dissociation constant
Bulk pH
Local pH
Curves represent bulk salt concentrations
pH = 7
pKa = 7
(Israels, Leermakers, Fleer. Macromolecules, 1994)

## Slide 27: Overview
Model
  SCF derivation
  Charge distribution coarse-graining
NFH Brush
  Validation using Srinivasan et al., 2014
  Conformational behavior and structure
Extensions
  Multiple peaks
  Binary NF brush
  Local pH consideration
Conclusions

## Slide 28: Conclusions
We have successfully applied our framework to single-component brushes of NFH when local pH is not a factor
Drastic changes in NFH height at low ionic concentrations are due to a second-order phase transition from 2C-coil to 2C
Further collapse can be explained by a first-order phase transition from 2C to 1C
Blocks determined by cumulative charge coarse-graining can give insight on internal structure
A multitude of subsequent projects can be addressed with minor adjustments to the framework (e.g., multi-chain, dissociation reactions, self-energy, etc.)

## Slide 29: Thank you!