## Slide 1: Nafion

## Slide 2: Motivation
Kodama et al. (2013) Electrochem. Commun. Kodama et al. (2018) ACS Catal.
For hydrogen fuel cells, Pt loading/efficiency is limiting factor for cost/efficacy
  Leading theory: Pt poisoned by adsorbed SO3 from ionomer at high operating V
However, scientific community has limited understanding of polymer physics
  Using polyelectrolyte brush SCFT can provide physical insights as well as computational framework for rational design of PEM ionomers
Relevant experiments:
SO3 adsorption measured by cyclic voltammetry (CV) – 0.100 M HClO4
  Apply potential at some scanning rate, measured current corresponds to interaction at electrode (e.g., reaction, adsorption)
(top) As humidity decreases, more current at lower voltage
  Thus, as ionomer—Pt distance decreases, more SO3 adsorption
(bottom) Long ionomer sidechains (LC) more current than short sidechain (SC)
  Note: LD = long distance between ether/SO3H; discussion becomes muddled on effect
SO3 (ad/de)sorption

## Slide 3: System
Schematic/Simplified system:
Polymer brush immersed in solution
Solution in contact with positively charged electrode
In real fuel cell:
Proton source from splitting of hydrogen (cathode, far left of schematic)
Proton sink from reaction with oxygen at Pt, forming water (anode, right side of schematic)
In CV experiments:
Pt coated with thin film of ionomer immersed in solution of 0.100 M HClO4
Preliminary SCFT model:
Grafted polymers are Nafion sidechains “grafted” onto the bulk ionomer membrane
  In the future, this can be extended to consider entire Nafion chains to more accurately describe poisoning mechanism
+++++++++++
−
−
−
−
−
−
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Backbone
Sidechain

## Slide 4: Sidechain only (Continuous Gaussian Chain)
Ionic strength 0.100 M
Model: “grafting surface” is bulk membrane/thin film; only considering elasticity of sidechains
True grafting density unknown, 7.31 c/nm2 is approximately the density of sidechains based on the random walk of its backbone
Left: Density of polymer on Pt surface as a function of membrane–Pt separation distance. Colors indicate Pt surface charge density
Right: Polymer density distributions (solid) and proton distributions (dotted) for D = 2.5 nm and grafting density 7.31 c/nm2. Density distribution of sulfonate block is dashed.

## Slide 5: Sidechain only (Continuous Gaussian Chain)
0.100 M
Discussion
In CV data, reaction goes to completion by 0.5 V (vs. RHE)
  Surface charge ~10 uC/cm2 according to Saha & Zenyuk. JPCC. 2021.
(Top) SCFT free energies as a function of D.
  (Top right) Free energies for 1—10 uC/cm2 colored. Small D is favorable at low charges, becomes unfavorable as surface charge reaches ~7 uC/cm2
(Bottom right) Normalized contributions of free energy for 1—10 uC/cm2. As surface charge increases, electrostatic interactions outweigh elastic penalties. At 10 uC/cm2, elastic penalties become dominant.

## Slide 6: Notes
\
SWITCH TO DGC SOON – thread dne bead-spring at N = 2

## Slide 7: Other
1e−07 M (pH 7)
Stretching to 4 nm shouldn’t be possible—artifact of CGC?