## Slide 1: NLH Update

## Slide 2: Although the height for pNFM is too short for low Cs, these curves are the best fit

## Slide 3: Analysis of other pNFM fitting paramters
b: Kuhn’s monomer length
v: Kuhn’s monomer volume
Degree of coarse graining
Charge of phosphorylated sites
chi: Flory-Huggins parameter (based on amino acid)
  Not shown below; made curves worse

## Slide 4: b and v values : Comparison of heights at 3 mM (solid lines) and 50 mM (dashed)
b = 2.0 nm
b = 3.0, v = 2.0 used for results on prev. slide

## Slide 5: Finer coarse-graining makes little difference
Finer
Note: This is also a demonstration that the coarse-graining is pretty good and finding appropriate the most appropriate blocks

## Slide 6: Degree of phosphorylation (-2.0e instead of -1.5e) also similarly little difference (not many units)
Affected blocks

## Slide 7: Results
Notes:
b and v values between non- and phosphorylated NFH and NFM are the same; only difference is charge distribution
-1.5e used for charge of phosphorylated sites
Same chi values for each amino acid were used for all results

## Slide 8: There are no significant differences between pNFM (left) and NFM (right).
Stronger shoulder
mM ionic strength
Very few phosphorylation sites on NFM, leading to little difference

## Slide 9: pNFH (left) and NFH (right) are extremely different
In contrast to NFM, NFH has very many phosphorylation sites.

## Slide 10: pNFH chains fold back after block 2 to form the inner condensed layer
Block 1
Block 2
Block 3
Remaining look like Block 3

## Slide 11: A fraction of pNFH chains do not fold back, forming the outer dilute layer
Block 2
Block 4
Block 6
Block 3
All dilute layers start with a distinct peak formed by Block 3. This is the region of KsP repeats

## Slide 12: Thus, pNFH chains (at low ionic strengths) look something like this
Crude schematic—I can try to make it look better later
2nd Block (red) either folds back or extends
3rd Block (blue) collects at interface between dilute and condensed layers
Block 2
Block 3

## Slide 13: The intrinsic difference between NFM and NFH (besides charge) lies in the chemical structures of the constituent amino acids
b = 4.00 nm
Higher fraction of stiffer residues
b = 0.50 nm
Lower fraction of stiffer residues
Increasing stiffness