## Slide 1: [WIP] NF Results
Last updated: 04/05/2024

## Slide 2: Problem
Neurofilament-derived brush comprised of one or more of:
  Light (156 residues) sidearm
  Medium (438 residues) sidearm
  Heavy (647 residues) sidearm
Response to ionic strength characterized by brush height measured through AFM
Question: role of each sidearm on overall morphology of brush and translation to biological neurofilaments

## Slide 3: Model
Interactions
Self-consistent field theory for charged multiblock macromolecules
  Coupled system of 5 algebraic equations and 2 partial differential equations
Elastic energy
Flory-Huggins (Hydrophobicity)
Electrostatics

## Slide 4: Treatment of Sequences
Protein  Multiblock charged macromolecular model
Coarse-graining by grouping similar neighboring charges (cusum method)
Yokokura et al. Biomacromolecules. 2024

## Slide 5: Coarse-grained Distributions (1 of 2)
Non-phospho
Phospho
NFL
NFM
NFH
Note: phospho chosen for best agreement with experimentally measured heights

## Slide 6: Coarse-grained Distributions (2 of 2)
Non-phospho
Phospho
NFM S1
NFM S2
NFH D2
NFH D6
Note: phospho chosen for best agreement with experimentally measured heights
—
—

## Slide 7: Agreement with AFM-measured heights
Unmodified
Modified
Chosen for best agreement with experimentally measured heights: . phospho H, . Thresh

## Slide 8: Effect of Sequence on Morphology (Unmodified proteins)
Bimodal (peaks at Block 3 & 7) charge distribution creates shoulder
Progressively increasing charge distribution extends tail
Non-phospho nearly net-neutral charge
Block 2 repels phospho. Block 3 (KSP units), preventing total collapse of outer layer

## Slide 9: Effect of Sequence on Morphology (Modified proteins)
Densities normalized to compare different proteins on same plot