## Slide 3: SCFT Build-up
Main Assumptions:
Chains within brush identical
Ion correlations neglected
Finite ion volume neglected
+
-
s
s
+
-
s
s
s
s
+
-
s
s
s
s
+
+
+
-
-
-
+
s
Main Interactions:
Monomer-monomer elasticity
Solubility (solvent-monomer)
Electrostatics (ion-monomer)

## Slide 4: SCFT Build-up
Result:
Generated fields (equations) that all particles in the system experience are continuous functions that depend in a mean-field way on all other particles (Andelman, 2006)
  “Self-consistent field theory” (SCFT)
+
-
s
s
+
-
s
s
s
s
+
-
s
s
s
s
+
+
+
-
-
-
+
s

## Slide 5: Model – SCF Review
Goal: Adapt framework for free polyelectrolyte in solution to model end-grafted protein brushes in solution
Interactions:
  Elastic entropy following Gaussian statistics
  Flory-Huggins 2-body interactions
  Incompressibility
  Electrostatics, ignoring any correlations

## Slide 6: Model – SCF Review
Semicanonical partition function
  Canonical in polymer, grand canonical in ions and solvent
Particle-to-field transformations
Hubbard-Stratonovich transformation
Saddle-point approximation
Block copolymer approximation

## Slide 7: Model – SCF Review
Variational Free Energy
  After statistical average over grafting surface (x-y plane)
Functional Minimization
SCF Equations

## Slide 8: Model – SCF Review
Satisfied Equations
  Mean-field Poisson-Boltzmann Equation
  Modified Diffusion Equation
Block K
Block 2
Block 1

## Slide 9: Model – Coarse-graining Method
Coarse-graining performed by grouping charges based on contributions to the slope of the cumulative charge
  Hyperparameters: Number of bins, Minimum number of AA per block
Sample sequence:
  HHHHHHHHHHHHHHH DDDDDDDDDDDDDDDDDDDDDDDDDDDDDD KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK KDDDHHK

## Slide 10: NFH Brush – Internal Structure
How does internal structure affect response to salt concentration?
Dramatic collapse
Cooperative collapse