## Slide 1: Nafion
Last updated 06/21/2024

## Slide 2: Motivation
Kodama et al. (2013) Electrochem. Commun. Kodama et al. (2018) ACS Catal.
For hydrogen fuel cells, Pt loading/efficiency is limiting factor for cost/efficacy
  Leading theory: Pt poisoned by adsorbed ionomer SO3 at high operating V
However, scientific community has limited understanding of polymer physics
  Using polyelectrolyte brush SCFT can provide physical insights as well as computational framework for rational design of PEM ionomers
Relevant experiments:
SO3 adsorption measured by cyclic voltammetry (CV) – 0.100 M HClO4
  Apply potential at some scanning rate, measured current corresponds to interaction at electrode (e.g., reaction, adsorption)
(top) As humidity decreases, more current at lower voltage
  Thus, as ionomer—Pt distance decreases, more SO3 adsorption
(bottom) Long ionomer sidechains (LC) more current than short sidechain (SC)
  Note: LD = long distance between ether/SO3H; discussion becomes muddled on effect
SO3 (ad/de)sorption

## Slide 3: System
Schematic/Simplified system:
Polymer brush immersed in solution
Solution in contact with positively charged electrode
In real fuel cell:
Proton source from splitting of hydrogen (cathode, far left of schematic)
Proton sink from reaction with oxygen at Pt, forming water (anode, right side of schematic)
In CV experiments:
Pt coated with thin film of ionomer immersed in solution of 0.100 M HClO4
Preliminary SCFT model:
Grafted polymers are Nafion sidechains “grafted” onto the bulk ionomer membrane
  In the future, model can be extended to consider entire Nafion chains to more accurately describe poisoning mechanism
+++++++++++
−
−
−
−
−
−
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
Backbone
Sidechain

## Slide 4: Model
Interactions
Self-consistent field theory for charged multiblock macromolecules
  Coupled system of 5 algebraic equations and 2 partial differential equations
  For sidechain-only system, 2 blocks; Block 2 contains -1e for SO3-
    F-H parameters taken from literature (Wu, Paddison, Elliot, Energy Env. Sci. 2008. 1. 284-293)
Elastic energy
Flory-Huggins (Hydrophobicity)
Electrostatics

## Slide 5: Sidechain only (Continuous Gaussian Chain)
Ionic strength 0.100 M
Model: “grafting surface” is bulk membrane/thin film; only considering elasticity of sidechains
True grafting density unknown, 7.31 c/nm2 is approximately the density of sidechains based on the random walk of its backbone
(Left) Density of polymer on Pt surface as a function of membrane–Pt separation distance. Colors indicate Pt surface charge density
(Right) Polymer density distributions (solid) and proton distributions (dotted) for D = 2.49 nm. Density distribution of SO3 bead is dashed.

## Slide 6: Sidechain only (Continuous Gaussian Chain)
0.100 M
In CV data, reaction goes to completion by 0.5 V (vs. RHE)
  Surface charge (metal) ~10 uC/cm2 according to Saha & Zenyuk. JPCC. 2021.
(Top) SCFT free energies as a function of D.
  (Top right) Free energies for 1—10 uC/cm2 colored. Small D is favorable at low charges, becomes unfavorable as surface charge reaches ~7 uC/cm2
(Bottom right) Normalized contributions to free energy for 1—10 uC/cm2. Contributions that equal 1 at D = 2.0 are the dominant interactions.
  U: Hydrophobicity; W+S: Elastic/Polymer; Electrostatic
  For < 10 uC/cm2, electrostatic interactions outweigh elastic penalties and lower D is favorable. At 10 uC/cm2, elastic penalties become dominant and higher D is favorable.
  Takeaway: competition between elastic stretching of sidearms and electrostatic attraction balances at 7 uC/cm2 (very roughly 0.5 V)

## Slide 7: Counterion only; NBC—(D)—NBC validations
sigma = -5e-20 C/nm2
Log-divergence, exact as lx  infty
sigma = -10e-20 C/nm2
sigma = -20e-20 C/nm2
Method: NBC left, NBC right, DBC somewhere

## Slide 8: Prelim results (20240906)
RH = 10%, sigma=1.35 nm-2
Lpha = 0.6 nm
Lpha = 1.0 nm
dz = 0.05
dz = 0.02

## Slide 9: Counterion only; DBC—NBC validations
Method: Newton iteration (a = 0.8), DBC right, NBC left

## Slide 10: Counterion only; (t) NBC—NBC validations
T = 1.0; Nt = 20,000
Method: Heat. SS at gradient change zero. Nested newton iteration. NBC right, NBC left. psi(0) = 0 shifted.
T = 1.0; Nt = 20,000
T = 1.0; Nt = 20,000
T = 1.0; Nt = 20,000
Doesn’t properly reflect slope 0. Abandoned

## Slide 11: Time in “Heat”
N = 1000
N = 5000
Total T, const Nt
dT, const Total T
Total T, const dT
Doesn’t properly reflect slope 0. Abandoned

## Slide 12: Uneven grid (theory)
Mapping theory
FD equations

## Slide 13: Uneven grid (analytical compare)
Dotted:
Infinite boundary condition, log-divergence
Srinivasan et al. Part I. 2024. Langmuir
Note: midpoint concentration can be calculated analytically but wasn’t quite right. In plot, used midpoint concentration obtained with N = 10,000
Dashed:
Finite boundary condition

## Slide 14: Uneven grid (N)
N = 50
N = 100
N = 250
N = 500
N = 1000
Transition knee in red (z ~ 90)
Analytical dotted
Analytical = log-divergence (original)

## Slide 15: Uneven grid (Lx, left)
L = 100
(N=1000)
L = 200
(N=1471)
L = 500
(N=2884)
Original
Extend left (evenly)
L = 50
(N=764)
Chop from left
s = −20e-20

## Slide 16: Uneven grid (Lx, right)
L = 100
(N=1000)
L = 101
(N=1051)
L = 110
(N=1508)
Original
Extend right (evenly)
L = 95
(N=746)
Chop from right
s = −20e-20

## Slide 17: Uneven grid + homo “polymer” (neg/pos surf)
s = −1e-20
s = +1e-20
Homo charge
s = −5e-20
s = +5e-20
Homo charge
s = −10e-20
s = +10e-20
Homo charge