## Slide 1: Nafion

## Slide 2: System
Simple picture:
Polymer brush immersed in solution
Solution in contact with positively charged electrode
In real fuel cell:
Proton source from splitting of hydrogen (cathode)
Proton sink from reaction with oxygen at Pt, forming water (anode)
In CV experiments:
Solution of 0.100 M HClO4
+++++++++++
−
−
−
−
−
−
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+

## Slide 3: Motivation
Kodama et al. (2013) Electrochem. Commun. Kodama et al. (2018) ACS Catal.
Pt poisoned by adsorbed SO3 from ionomer
  Pt loading/efficiency is limiting factor for fuel cells
Scientific community has limited understanding of polymer physics
Adsorption measured by cyclic voltammetry (CV) – 0.100 M HClO4
  Apply potential at some scanning rate, measured current corresponds to interaction at electrode (e.g., reaction, adsorption)
(top) As humidity decreases, more current at lower voltage
  As ionomer-Pt distance decreases, more adsorption
(bottom) Long sidechains (LC) more current than short sidechain (SC)
  Discussion on long distance between ether/SO3H (LD) becomes muddled

## Slide 4: Sidechain only (Continuous Gaussian Chain)
Ionic strength 0.100 M
Model: “grafting surface” is bulk membrane/thin film; only considering elasticity of sidechains
True grafting density unknown, 7.31 c/nm2 is approximately the density of sidechains based on the random walk of its backbone
Left: Density of polymer on Pt surface as a function of membrane–Pt separation distance. Colors indicate Pt surface charge density
Right: Polymer density distributions (solid) and proton distributions (dotted) for D = 2.5 nm and grafting density 7.31 c/nm2. Density distribution of sulfonate block is dashed.

## Slide 5: Sidechain only (Continuous Gaussian Chain)
0.100 M
Discussion
In CV data, reaction goes to completion by 0.5 V (vs. RHE)
  Surface charge ~10 uC/cm2 according to Saha & Zenyuk. JPCC. 2021.
(Top right) Comparing SCFT free energies, small D favorable at low charges, becomes unfavorable as surface charge reaches 7 uC/cm2
(Bottom right) Attraction (lower F when decreasing D) caused by electrostatics dominating. Repulsion caused by elastic interactions dominating.

## Slide 6: Notes
\
SWITCH TO DGC SOON – thread dne bead-spring at N = 2

## Slide 7: Other
1e−07 M (pH 7)
Stretching to 4 nm shouldn’t be possible—artifact of CGC?