## Slide 1: Polymer SCFT for Studying Ionomer Morphology in PEMFCs
07/22/2024
Takashi Yokokura, Wang Group

## Slide 2: Ionomer morphology underlies key questions in PEMFCs
Confinement effects
Pt poisoning mechanism
Sidechain effects
Shirvastava et al. Macromolecules 2018, 51, 9839−9849; Kusoglu et al. Adv. Funct. Mater. 2016, 26, 4961–4975; K. Kodama et al. Electrochemistry Communications 36 (2013) 26–28
Hydration / Humidity
How do we optimize PEMFC structure?
How do we optimize PEMFC operation?

## Slide 3: Ionomer morphology underlies key questions in PEMFCs
Pt poisoning mechanism
Confinement effects
Sidechain effects
Shirvastava et al. Macromolecules 2018, 51, 9839−9849; Kusoglu et al. Adv. Funct. Mater. 2016, 26, 4961–4975; K. Kodama et al. Electrochemistry Communications 36 (2013) 26–28
Hydration / Humidity
How do we optimize PEMFC structure?
How do we optimize PEMFC operation?
We seek to provide molecular details underlying complex polymer morphologies by developing and applying robust theories.

## Slide 4: Outline
Overview of polyelectrolytes
  What are the key interactions that need to be accounted for?
  Why is the interplay between these interactions important?
  What kind of insight can theory provide for polyelectrolyte systems?
Brief derivation of our self-consistent field theory
  What are the key equations for studying the morphologies of PEMs?
Proposal for application to Ionomer—Pt interface
  What can our theory provide on the mechanism of Pt poisoning?

## Slide 5: Outline
Overview of polyelectrolytes
  What are the key interactions that need to be accounted for?
  Why is the interplay between these interactions important?
  What kind of insight can theory provide for polyelectrolyte systems?
Brief derivation of our self-consistent field theory
  What are the key equations for studying the morphologies of PEMs?
Proposal for application to Ionomer—Pt interface
  What can our theory provide on the mechanism of Pt poisoning?

## Slide 6: Polyelectrolyte behavior is controlled by three main interactions
Electrostatics (repulsion) – charged monomeric groups and dissolved salt ions
Elasticity – polymer chains are formed by a series of connected monomers
Hydrophobicity (attraction) – van der Waals interactions between monomers and solvent
Monomer
Solvent
The relative strengths of these interactions are determined by monomer chemistry (e.g., backbone, sidechain EW, etc.) and environment (e.g., temperature, humidity)

## Slide 7: These interactions dictate polyelectrolyte morphology
Competition between hydrophobicity, long-range electrostatics, and polymer elasticity can lead to complex morphologies
Example: moderately charged brushes for decreasing hydrophobicities
Fully condensed
(Attraction-dominated)
Fully swollen (Repulsion-dominated)
Polymer density distributions from SCFT
Corresponding schematic (insight)
Microphase segregated

## Slide 9: Outline
Overview of polyelectrolytes
  What are the key interactions that need to be accounted for?
  Why is the interplay between these interactions important?
  What kind of insight can theory provide for polyelectrolyte systems?
Brief derivation of our self-consistent field theory
  What are the key equations for studying the morphologies of PEMs?
Proposal for application to Ionomer—Pt interface
  What can our theory provide on the mechanism of Pt poisoning?

## Slide 10: Our SCFT systematically includes these coupled interactions
Elasticity (Gaussian chain)
Polymer path
Local polymer volume fraction
Local solvent volume fraction
Local charge density
Coulomb operator (PB equation)
Hydrophobicity (Flory—Huggins)
Long-range electrostatics

## Slide 11: Self-consistent field equations provide microscopic details
Particle-to-field and Hubbard—Stratonovich transforms, saddle-point approximation, functional minimization
Interactions
Self-consistent Field Equations
For PEMs, we are most interested in polymer, sidechain, and proton distributions
System
(e.g., const. number of polymers, system connected to bulk solvent and salt solution)

## Slide 12: Outline
Overview of polyelectrolytes
  What are the key interactions that need to be accounted for?
  Why is the interplay between these interactions important?
  What kind of insight can theory provide for polyelectrolyte systems?
Brief derivation of our self-consistent field theory
  What are the key equations for studying the morphologies of PEMs?
Proposal for application to Ionomer—Pt interface
  What can our theory provide on the mechanism of Pt poisoning?

## Slide 13: Rudimentary proof-of-concept: considering sidechains only
Model: “grafting substrate” is the “bulk” thin film. Sidechains are uniformly tethered to the surface.
Polymer density distributions illustrates the effect of Pt surface charge density on thin-film morphology
  As charge increases, the degree of polymer poisoning increases
    The vast majority of the density near Pt is composed of SO3− (dashed)
  Proton distributions (dotted) illustrate the competing effects between increased (+) surface charge density and the ion cloud surrounding the SO3− groups
However, this model does not account for the rest of the film (e.g., elasticity of the ionomer backbones)

## Slide 14: Proposed system for Ionomer—Pt interface at varying humidities
Pt
Entire ionomer chains (backbone + sidearms)
Ions
Water (liquid)
Effects on ionomer morphology by
  Water uptake (e.g., number of water molecules)
  Pt potential
  Ionomer chemistry
    Equivalent weight, sidechain length, etc.
Our SCFT would provide
  Polymer/Sidechain density distributions
  Proton distributions
  Mechanisms underlying morphological changes